## Slide 1
Tungsten Source Spectroscopy for the ITER-Like Wall on JET
S. Brezinsek
G.V Rooij, J.W. Coenen
A.G. Meigs, M. Stamp, R. Dux and JET-EFDA Contributors
ADAS Workshop, Cadarache, 24.9.-25.9.2012

## Slide 2: Outline
ITER-Like Wall at JET: Installation, Key Results and Issues related to W components
W Source Quantification
  Spectroscopic Transitions
  Dependence on Plasma Conditions
  Prompt Redeposition
Summary

## Slide 3: Metallic Walls: ITER-Like Wall at JET
Change in operational space
  Need for better plasma control
  Need for heat load mitigation schemes
ITER-material mix used for the first in a tokamak
“Carbon-free” environment
  Reduced migration to remote areas
  Reduced tritium retention
  Loss of carbon as main radiator
ITER
JET
Demonstrate low fuel retention, migration
and possible fuel recovery
Demonstrate plasma compatibility
with metallic walls
Main goals of the ILW experiment
Input to the decision about the first ITER divertor
V. Philipps
FED 2011
G. Matthews
Phys. Scripta 2011
Notes: NBI upgrade in parallel

## Slide 4: ILW completed: 8th May 2011
Tungsten
Beryllium
Be limiter
bulk
W divertor
Total: 2t of Be installed
Total: 2t of W installed
ITER-wall material combination, but only inertial cooled plasma-facing components
New energy and power load limitations imposed with respect to JET-C
Notes: Figure W-coated CFC

## Slide 5: Residual Carbon and Oxygen
Main chamber CIII and outer divertor CII edge fluxes:
Residual C dropped with ILW installation by one order of magnitude
Dedicated JET-C/JET-ILW comparison pulses show a drop of about a factor 20
Oxygen gettered by Be, but still present at low levels in the plasma
Comparable C reduction also observed in core and edge concentrations by CXRS
Averaged Zeff dropped from 1.9 (JET-C) to 1.2 (JET-ILW)
S. Brezinsek
PSI2012
x20

## Slide 6: Key Result: Long Term Fuel Retention
Reduction of fuel retention rate with JET-ILW just in line with ITER-predictions!
Lower fuel content in Be co-deposits in comparison with C co-deposits
Note post mortem analysis shows typically a factor ~4 lower retention in comparison with gas balances => tile extraction end of year => post mortem analysis
ITER D-T discharges (400s)
time [s]
T retention rate [T/s]
JET gas balance measurements
x10
S. Brezinsek
IAEA 2012
JET

## Slide 7: Key Result: Stable H-mode Operation
Type I ELMy H-modes achieved in low
and high triangular plasma with NBI
Operational window is smaller and requires
  Gas fuelling (to reduce W source)
  Minimum ELM frequency (to flush W)
  Central heating (to avoid peaking)
otherwise W-accumulation can occur
Stable ELMy H-mode at D injection rates G≥ 0.5x1022/s with H98~1 (Ip=2.5 MA, Bt=2.5 T)
  ELM flushing successful at f>10Hz
  W concentration below CW~5x10-5
13
14
15
16
17
18
nC [1019 m-3]
bN
H98y2
Ha [a.u.]
PNBI, PICRH
PRAD, [MW]
time [s]
Pulse 82240 IP=2.0MA, BT=2.1T, Zeff=1.2
E. Joffrin
IAEA2012
Notes: One profile from HRTS to show regime

## Slide 8: Issue: W Transport and Accumulation
ELM frequence too low
W peaking
Sawteeth die out
W accumulation
Temperature collapse
81913
Te (keV)
Power (MW)
JET-ILW
PNBI
Time(s)
Te (0)
Te (~0.85)
Prad bulk
Prad tot
peaking
accumulation
S Brezinsek
EPS 2012

## Slide 9: Issue: W Cluster Release
temperature [keV]
power [MW]
time [s]
JET-ILW #81765
Te (0)
Te (~0.6)
W cluster (~0.1mm) released from divertor => Usually not harmful, but cool plasma down
Number of events reduced with operational time => Thermal fatigue of components not cause
W cluster
18
20
22
G. Matthews
PSI2012
VUV

## Slide 10
W?
W Sources in JET
Strong W source (outer divertor) critical issue:
  Radiative cooling and W accumulation
  Limit lifetime of W plate by erosion
Best plasma performance in JET-CFC obtained in
  Plasmas with low density in the divertor
  Plasmas showed large ELM energy drop
Not possible with W divertor
  Low density means high Te and energy of impinging ions => strong W sputtering
  Large ELMs carry high energy ions
  => melting and sputtering of W possible
Needs best compromise:
  Low W sputtering
  High W divertor retention
  Small ELMs to flush confined W

## Slide 11: W Source Distribution
W source distribution
W source spectroscopy
W sputtering
=> In divertor
mainly
by impurities!
Local cooling (low Te)
Surface effects (nitrides?)
Impinging impurity mixture (Be, O, C)
Ionisation stage of impurities
Impinging ion and deuterium flux
ERO modelling
Modelling of WI and WII lines photon efficiencies: GW=S/XB fW
Modelling of WF6 injection
Calibration by WF6 injection
TEXTOR & PSI-2

## Slide 12: W Source Spectroscopy
Divertor plasma
W+ *
W target plate
Zimp
W
W+
ne, Te increase
Y
S
S′
W*
X
B
WI
WII
Full ionising plasma conditions
W sputtering flux from neutral
W line observation
S for ioniSation rate coeffecient
X for eXciatation rate coeffecient
B for Branching ratio
Accordingly for the flux of single
ionsed W
Comparison of GW0 and GW+
=> prompt redeposition factor
G.v.Rooij PSI 2012

## Slide 13: Grotian Diagramm for Neutral W
NIST tables version 3
line
ratios
f(T
e
)
line
ratios
f(T
W
)
wave numbers / cm-1
1eV8066 cm-1
»
0.5eV
population mechanisms:
e-collisions from ground state
cascades from upper levels
Which transition should or can be observed? S/XB values?

## Slide 14: Example Lines from TEXTOR
No difference in line shape of different WI and WII lines
Line ratios of WI lines with same lower level comparable
WII lines measured and quantified in WF6 injections
S. Brezinsek Phy. Scripta 2011
Main favourites for JET: WI at 400.875nm and UV lines
Alternative lines to weak or blended by impurites from Be, C, Ar, N etc.

## Slide 15
S/XB for WI lines
WI @ 400.9nm
WI @ 429.5nm
D. Kondratjev GKU

## Slide 16: Photon Efficiencies
WI at 400.9nm best documented line
Multimachine fit of S/XB values applied for quantification of W fluxes
Contrast to AUG which uses constant 20 (but works in the range od 5-15 eV)
JET outer divertor hotter and has larger ELM energy drops (higher Te)
Different methods:
Weight loss
Spectroscopy
WF6 injection
W(CO)6 injection
S. Brezinsek ITPA 2012

## Slide 17: Direct Imaging Spectrometer in JET
A. Meigs PSI 2012
Line-of-sight
UV –NIR system: three spectrometers
250nm -1100nm
up 30 nm coverage per system
300 / 600 /1200 l/mm gratings
Spatial coverage of 360 mm
Spatial resolution: 1.8cm
Time resolution: 40ms

## Slide 18: W Sputtering – L-mode
Low recycling regime (steady-state):
W sputtering decreases with density increase and temperature decrease
Impact of flux increase to the target
compensated by drop in temperature
Sputtering caused by impurity ions
(here: Be ions)
W source in the outer divertor
Te=45eV
Te=35eV
Te=25eV
S. Brezinsek EPS2012

## Slide 19: W Sputtering Yields
AUG-W
JET-ILW
Increasing N
Divertor plasma cooling by deuterium fuelling or by deuterium+nitrogen seeding leads to reduction of W source => below phys. sputtering threshold
Competition between higher impurity flux and local cooling in seeded discharges
Inter-ELM and steady-state regimes with low Te and low W sputtering achieved
L. Aho-Mantilla
PSI2012
J.W. Coenen
PSI2012

## Slide 20: W Sputtering – H-mode
JET: 13 MW NBI, ne =7.5·1019 m-3, 10 Hz ELMs
ASDEX: Dux et al., J Nucl Mat 390–391 (2009) 858
        Factor 8 between inter- and intra-ELM sputtering
Similar ratio for JET Te=20 eV and AUG Te=6 eV
Erosion during ELMs dominate at high densities
average
between ELMs
G.v. Rooij PSI2012

## Slide 21: Prompt Redeposition
Divertor plasma
W+ *
W target
W
W+
ne, Te increase
Y
S
S′
W*
X
B
WI
e.g. 400.9 nm
WII
e.g. 364 nm
X′
B ′
 B
W+
rL
lion
W0
JET
G. v. Rooij PSI2012
Zimp

## Slide 22: Example: Divertor UV – Spectra in JET

## Slide 23
Ratio of WII / WI
Factor 2 change indicates >50% redeposition
Textor same result at same Te and ne
S. Brezinsek et al., Phys. Scr. T145 (2011) 014016.
41018 m-3, 50 eV:
1.41019 m-3, 50 eV:
G. v. Rooij PSI2012

## Slide 24: Summary
ILW installed in JET and in operation
  Low fuel retention measured
  Good plasma performance in H-mode obtained, but operational window narrow
  W peaking and accumulation can occur => avoidance by optimisation
W sputtering measured by optical spectroscopy
  WI at 400.9nm used – other lines measured
  W sputtering as function of impurity composition, impinging flux and temperatures characterised in L-mode
  W sputtering by ELMs dominate
  Prompt redeposition of W measured by WI and WII line ratio analysis

## Slide 25: Change in Impurity Composition
ne =
1.6·1019 m-3
2.0·1019 m-3
2.8·1019 m-3
1 MW NBI ramp
0.5% Be2+
ne = 1.6·1019 m-3
3 MW ICRH
2 MW ICRH
1 MW ICRH
3 MW ICRH
2 MW ICRH
1 MW ICRH
3 MW ICRH
2 MW ICRH
1 MW ICRH
ne = 2.0·1019 m-3
ne = 2.8·1019 m-3
1 MW 2 MW 3 MW
Be fraction doubles in each step
Effect of steps in power in line with Be impurity variation
Sputtering yield ~quadruples in each density step

## Slide 26: H-mode Pedestal and Impurity Seeding
JET-ILW D2 fuelling type I ELMs
JET-C D2 fuelling
JET-ILW D2 fuelling type I ELMs
JET-C D2 fuelling
JET-ILW D2 + N2 seeding
Te, ped [keV]
ne,ped [1019m-3]
JET-ILW boundary for type I ELM below type III boundary for JET-C
Nitrogen seeding restores pedestal and temperature regime
C. Giroud IAEA2012
H-mode pedestal is colder with JET-ILW in comparison to JET-C
L. Frasinetti P4.072

## Slide 27: Example: Monitoring Discharge
ohmic
L-mode
H-mode
limiter
aux. power
density
Identity plasmas repeated regularly to document wall conditions
Monitor status of impurities (Be, C, O, Ar, N, W) with operational time
S. Brezinsek
EPS 2012

## Slide 28
S/XB for WI and WII lines
WII @ 434.8nm
WI @ 522.5nm
Comparison with experimental data from JET
in preparartion
New W data (in ADAS) should be compared
D. Kondratjev GKU

## Slide 29: Be Impurities in the Divertor
K. Krieger
PSI2012
Measure and simulate initial start-up situation with Be/W material mix
First wall Be erosion by impinging ions => transport in the scrape-off layer
=> deposition in the W divertor => material mixing
Be deposition in both legs, but initial Be contamination from limiter plasmas
BeII 527nm
Be flux in the divertor after first 1000 plasma seconds
W divertor target plates
Vessel walls
PFR
Separatrix
BB
SOL flow
deposition
Be net erosion
deposition
/ erosion
Ion flux